## Slide 1
Dr. Chris Chiu
Chitec Technology
Presented by
Christopher J. Karwowski
New Advances in 2nd Generation Light Stabilizers Functionality for the Coatings Industry
Pacific Northwest Society of Coatings Technology CoatingsFest
Victoria, British Columbia
October 11th, 2018

## Slide 2
Pollution lies in the shadow of civilization.

## Slide 3: 2017 European Coatings Poll
50% of the attendees indicated that
water-borne technology is
the most important future technology
for the coating industry.

## Slide 4: Water-borne (WB)
blank
A
C
B
blank
A
C
B
Outdoor initial
41 day
Water-borne (WB) technology is mature for interior coatings. Exterior Coatings are still evolving with research moving toward high performance durability similar to solvent systems.

## Slide 5: Photo-oxidation pathway
1st Line of Defense : UVA
2nd Line of Defense: Quencher
3rd Line of Defense: HALS
“Ice cube”
“Heat barrier”
“Extinguisher”
280nm - 400nm

## Slide 6: Commodity WB UVA
Hydrophilic BTZ is a liquid BTZ UVA (see below) which has been formulated as the premier UV protector for WB coatings. Its hydrophilic nature allows it to be easily emulsified with or without hindered amine light stabilizer (HALS). However, in exterior coatings, it is only slightly better than nothing at all.
Hydrophilic BTZ
Solution

## Slide 7: Hydrophilic BTZ are not dependable
Many customers saw gaps between data performed by outdoor exposure and WOM.
Outdoor exposure
WOM
Why? We hypothesize acid rain contamination.

## Slide 8: Water flushing experiments
Flow rate: 1.8 L/min
PET film
Purpose | to mimic the rain fall flushing effect on UVA in the coatings.
Substrates | PET film or glass plate
Resin systems | Polyurethane dispersion (PUD) and water-borne acrylic (WBA).
UVA concentration | 0.1% by weight
Coatings thickness | 60 microns
Water flow rate | 1.8L/min
Temp. | 20-25 °C
QUV lamp | 340 nm
Cycle | QUV 48 hours followed by water-flushing 24 hours.

## Slide 9: UV absorbance show the life of UV absorber
Hydrophilic BTZ initial
Hydrophilic BTZ after flushed with water five cycles
25% loss of UVA

## Slide 10: Hydrophilic BTZ vulnerable to water flushing
After 15 cycles, nearly 1,000 hours, Hydrophilic BTZ lost more than 80% of its functionality. The result is expected due to the hydrophilic nature of Hydrophilic BTZ. However, the speed of loss is astonishing. Therefore, it is recommended that Hydrophilic BTZ should not be used in exterior applications that have exposure to rain.

## Slide 11: First generation of Chiguard® WB
Solid Hydrophobic BTZ was designed to prevent degradation issues with water flushing. It is a dispersion of solid BTZ UVA as shown below. It shows no apparent lose of UV absorbance after water-flushed for the first 2 cycles.
Solid Hydrophobic BTZ WB initial
Solid Hydrophobic BTZ WB
after 2 cycles

## Slide 12: Solid Hydrophobic BTZ
 | 1st G WB
Active ingredient | 20% (solid)
Inactive ingredients | 10-15%
Compatibility with resin | Low
Phase separation | 3 months min.
Production cost | High
Structure of the active ingredient | 

## Slide 13: Limit of First generation WB
The maximum dosage of Solid Hydrophobic is only 0.5%. More than 0.5% gives opaque appearance after baking.
PUD +
0.5% 1st G WB
PUD +
1% 1st G WB
PUD +
2% 1st G WB
PUD +
2% 2nd Generation BTZ

## Slide 14: 2nd Generation of WB UVA and WB HALS
 | 2nd Generation BTZ WB | 2nd Generation Hals WB | 2nd Generation Triazine WB
Active content | Liquid BTZ UVA | Liquid acid resistant HALS | Liquid TRZ UVA
Structure |  |  | 
Particle size | <500nm | <500nm | <500nm
Appearance | White milky emulsion | White milky emulsion | Pale yellow emulsion

## Slide 15: Chiguard® WB technology is a product of nanotechnology
Oily UV absorber
Emulsifiers
Cell wall destruction
Nano Micelles
Emulsifier A
Emulsifier B
Stabilizing nano size micelle is a result of 5 years overwhelming research work.

## Slide 16: Five years of R&D explained!
2 months heat stability test at 60 °C and cooling stability at 10 °C without phase separation. In other words, one test took 2 months to know it is good or not!
2nd Generation BTZ WB is stabilized in 60°C
A: The appropriate emulsification process achieve the excellent stability B: Inappropriate emulsification process, likely to cause oil and water separation
A
B

## Slide 17: Compatibility tests
Over 50 resins were tested for compatibility. If compatibility issue occurred, defects on coatings can be easily observed. Acrylic based UVA are more suspected to have compatibility issue.

## Slide 18: 2nd Generation WB vs. Competition
Only two companies in the world supply emulsified water-borne UVA, one is Chitec and the other BASF. Their technologies differ in how to stabilize the micelles. Chitec uses emulsifier cocktails and BASF relies on acrylic-based encapsulation*.
 | 2nd Generation WB LS | Competition
Active concentrations | 30% | 20-40%
Inactive concentrations | 1-3% | 10-20%
Stabilizing means | emulsifiers | Polyacrylates shell
*This process is covered by parent no. US 2006/0287416 A1, filed on Sept. 1, 2006.

## Slide 19: The advantage of inter-miscibility
2nd Generation BTZ, Hals, and Triazine WB Technology can be mixed in any ratio to generate a stable emulsion.
BTZ UVA
Triazine UVA
HALS
Mixing experiment
Stable emulsion

## Slide 20: The advantage of inter-miscibility
2nd Generation BTZ, HALS, and Triazine Water Borne Technology
Stable emulsion
Conditions after one month

## Slide 21: Life of 2nd G WB in WBA
BTZ WB and Triazine WB showed significant stability against water-flushing over Hydrophilic BTZ with or without HALS in WBA coatings system. Triazine UVA chemistry did not provide extended durability in this system.
Triazine WB
BTZ WB
Hydrophilic
BTZ / Hals WB
QUV340nm / pH:7 wash Test (hours)
UVA retention Acrylate QUV/pH:7
Chart: Abs. %
| 0 | 168 | 264 | 336 | 432 | 504 | 600 | 768 | 936
5400WB | 1 | 1.0143 | 1.0571 | 1.1 | 1.0286 | 1.05 | 0.95714 | 0.86429 | 0.72857
5582WB | 1 | 0.94737 | 0.94737 | 0.93684 | 0.91579 | 0.90526 | 0.88421 | 0.84211 | 0.76842
5530 | 1 | 0.81818 | 0.72727 | 0.74545 | 0.61818 | 0.52727 | 0.45455 | 0.30909 | 0.23636
5582/353 WB | 1 | 0.94545 | 0.94545 | 1.0364 | 0.89091 | 0.87273 | 0.81818 | 0.74545 | 0.65455

## Slide 22: Life of 2nd G WB in PUD
BTZ WB and WB indicate better durability in the PUD system against the Acrylate system under water-flushing treatment, HALS was able to increase the durability when used with BTZ WB as indicated.
QUV340nm / pH:7 wash Test (hours)
Triazine WB
BTZ WB
BTZ/Hals blend
Hydrophilic/Hals
UVA retention PU QUV/pH:7
Chart: Abs. %
| 0 | 168 | 336 | 408 | 504 | 576 | 672 | 840 | 1008
5400WB | 1 | 0.96825 | 0.95767 | 0.9418 | 0.9418 | 0.93122 | 0.89947 | 0.86772 | 0.84127
5582WB | 1 | 0.92857 | 0.91667 | 0.88095 | 0.86905 | 0.86905 | 0.80952 | 0.77381 | 0.70238
5530 | 1 | 0.85294 | 0.71569 | 0.62745 | 0.54902 | 0.4902 | 0.44118 | 0.36275 | 0.30392
5582/353 WB | 1 | 0.95455 | 0.92424 | 0.92424 | 0.90909 | 0.90909 | 0.86364 | 0.84848 | 0.81818
5530/353 | 1 | 0.86777 | 0.68595 | 0.61983 | 0.57025 | 0.52893 | 0.4876 | 0.43802 | 0.41322

## Slide 23: Life of 2nd G WB without water-flushing
Triazine WB
BTZ WB
Hydrophilic
BTZ WB/Hals
UVA retention Acrylate QUV340nm/Cond.
QUV340nm/Cond. Test (hours)

## Slide 24: Acid rain fall in the World

## Slide 25: Life of 2nd Generation WB in WBA under
Simulated Acid Rain flushing decreased the durability of UVA’s in the WB Acrylate system than Neutral pH water flushing as shown in the solid lines. However, the durability can be increased by adding HALS as shown on the purple line.
Chart: 
| 0 | 168 | 264 | 336 | 432 | 504 | 600 | 768 | 936
5400WB | 1 | 1.0143 | 1.0571 | 1.1 | 1.0286 | 1.05 | 0.95714 | 0.86429 | 0.72857
5582WB | 1 | 0.94737 | 0.94737 | 0.93684 | 0.91579 | 0.90526 | 0.88421 | 0.84211 | 0.76842
5530 | 1 | 0.81818 | 0.72727 | 0.74545 | 0.61818 | 0.52727 | 0.45455 | 0.30909 | 0.23636
5582/353 WB | 1 | 0.94545 | 0.94545 | 1.0364 | 0.89091 | 0.87273 | 0.81818 | 0.74545 | 0.65455
Chart: 
| 0 | 168 | 240 | 336 | 408 | 504 | 600 | 672 | 768 | 840 | 936 | 1104 | 1272
5400WB | 1 | 1.0451 | 1.0526 | 1.0602 | 1.0526 | 0.97744 | 0.96241 | 0.96992 | 0.88722 | 0.84211 | 0.7594 | 0.68421 | 0.57143
5582WB | 1 | 1 | 0.98592 | 0.97183 | 0.95775 | 0.92958 | 0.91549 | 0.90141 | 0.88732 | 0.88732 | 0.80282 | 0.70423 | 0.52113
5530 | 1 | 0.78351 | 0.75258 | 0.71134 | 0.69072 | 0.62887 | 0.65979 | 0.59794 | 0.53608 | 0.50515 | 0.46392 | 0.37113 | 0.25773
5582/353 WB | 1 | 1.0794 | 1.0635 | 1.0476 | 1.0794 | 1.0159 | 1.0794 | 1.0317 | 1 | 0.98413 | 0.93651 | 0.88889 | 0.84127
Abs. %
Triazine WB
BTZ WB
Hydrophilic
BTZ/Hals blend
QUV340nm / pH:4 wash Test (hours)
QUV340nm / pH:7 wash Test (hours)
Triazine WB
BTZ WB
Hydrophilic
BTZ/Hals blend
UVA retention Acrylate QUV/pH:4
Simulated Acid Rain flushing

## Slide 26: Life of 2nd Generation WB in PUD under
Surprisingly, Simulated Acid Rain flushing increased the durability of the Hydrophobic UVA’s in PUD to more than 90% in 1100 hours.
Earlier hypothesis would have expected a drop in durability instead of increasing.
Simulated Acid Rain flushing
Chart: 
| 0 | 168 | 336 | 408 | 504 | 576 | 672 | 840 | 1008
5400WB | 1 | 0.96825 | 0.95767 | 0.9418 | 0.9418 | 0.93122 | 0.89947 | 0.86772 | 0.84127
5582WB | 1 | 0.92857 | 0.91667 | 0.88095 | 0.86905 | 0.86905 | 0.80952 | 0.77381 | 0.70238
5530 | 1 | 0.85294 | 0.71569 | 0.62745 | 0.54902 | 0.4902 | 0.44118 | 0.36275 | 0.30392
5582/353 WB | 1 | 0.95455 | 0.92424 | 0.92424 | 0.90909 | 0.90909 | 0.86364 | 0.84848 | 0.81818
5530/353 | 1 | 0.86777 | 0.68595 | 0.61983 | 0.57025 | 0.52893 | 0.4876 | 0.43802 | 0.41322
Chart: 
| 0 | 168 | 240 | 336 | 432 | 504 | 672 | 744 | 840 | 1008 | 1176
5400WB | 1 | 1.0248 | 1 | 0.9901 | 0.9901 | 0.9703 | 0.9604 | 1.0297 | 0.96535 | 0.92574 | 0.90099
5582WB | 1 | 1.0405 | 1.0946 | 1.0541 | 1.0135 | 1.0405 | 0.98649 | 0.93243 | 0.94595 | 0.89189 | 0.86486
5530 | 1 | 0.86607 | 0.76786 | 0.66964 | 0.58929 | 0.53571 | 0.48214 | 0.45536 | 0.41964 | 0.36607 | 0.3125
5582/353 WB | 1 | 1.0169 | 1 | 0.94915 | 1.0339 | 1.0169 | 1 | 0.9661 | 0.94915 | 0.91525 | 0.88136
5530/353 | 1 | 0.84091 | 0.70455 | 0.60227 | 0.64773 | 0.61364 | 0.57955 | 0.56818 | 0.53409 | 0.48864 | 0.46591
UVA retention PU QUV/pH:4
Triazine WB
BTZ WB
Hydro
BTZ/Hals Bld
Hydro/Hals Bld
QUV340nm / pH:7 wash Test (hours)
Triazine WB
BTZ WB
Hydro
BTZ/Hals Bld
Hydro/Hals Bld
QUV340nm / pH:4 wash Test (hours)

## Slide 27: Summary
Chitec has introduced two 2nd generation WB UVA’s and one premier WB HALS which showed significant resistant to water-flushing. They are ideal for all water-borne applications.
Hydrophilic BTZ was washed away from coatings easily, so it is not recommended to applications exposure to heavy rain fall and including Acid Rain environment.
Simulated Acid Rain flushing decreased the durability UVA’s in WB Acrylate systems than water flushing. However, this can be overcome adding HALS.
Surprisingly, unlike water flushing, Simulated Acid Rain flushing increased the durability of the Hydrophobic UVA’s in PUD instead of decreasing the durability as expected.
In this testing PUD’s indicate to be more durable than WB Acrylate’s against Simulated Acid Rain testing based on the Simulated Acid Rain flushing experiments.

## Slide 28: Acknowledgement
Dr. Chris Chiu Ph.D Author
Heidi Lu
Milly Hung
The Outstanding R&D Chemists at Chitec Taiwan
The PNWSCT Technical Advisory Board