## Slide 1: Extender Functionality in Elastomeric Coatings
PNWSCT Coatings Fest, October 2018

## Slide 2: Challenges of a Changing World

## Slide 3: Elastomeric Coatings
Wall
Roof

## Slide 4
Elastomeric Coating Formulation
Can of Paint
Water
Filler
Additive
Pigment
Binder
INGREDIENTS | Pounds | Gallons
Water | 135.00 | 16.21
KTPP | 1.00 | 0.05
Dispersant | 8.00 | 0.91
Ammonium Hydroxide | 1.50 | 0.18
Surfactant | 2.00 | 0.24
Defoamer | 1.50 | 0.20
Preservative | 1.50 | 0.16
Titanium Dioxide | 100.00 | 3.00
Zinc Oxide | 20.00 | 0.43
Calcium Carbonate | 385.00 | 17.04
Biocide | 3.00 | 0.33
Emulsion | 530.00 | 58.89
Propylene Glycol | 18.00 | 2.08
Cellulosic Thickener | 4.00 | 0.48
Ammonium Hydroxide | 2.20 | 0.27
Defoamer | 2.00 | 0.27
Total | 1214.70 | 100.74
Density (lb/gal) | 12.06 | 
Weight % Solids (%) | 65.29 | 
Volume % Solids (%) | 49.89 | 
PVC (additive included) (%) | 40.72 | 
PVC (minus additive) (%) | 41.88 | 
PVC / CPVC | 0.60 | 

## Slide 5: Particle Morphology
Nodular
    Silica
    Calcium Carbonate
    Nepheline Syenite
Platy
    Muscovite Mica
    Talc
    Kaolin
Image reproduced from the 'Images of Clay Archive' of the Mineralogical Society of Great Britain & Ireland and The Clay Minerals Society.
Acicular
    Wollastonite

## Slide 6: Particle Size
0 μm
35μm
Calcium Carbonate
Titanium Dioxide
Wollastionite
Talc
Calcium Carbonate
Kaolin
Mica
Wollastionite
Silica
Silica
Nepheline Syenite
Mica
Talc,
Calcium Carbonate,
Nepheline Syenite

## Slide 7: Variations in Oil Absorption Should be Considered

## Slide 8: Critical Pigment Volume Concentration
PVC
Performance Values
CPVC
tensile
permeability
gloss
Fraction of Critical = PVC/CPVC
  PVC = 100 * Vp/ (Vp + Vnvb)
  Vp = pigment and filler volume
  Vnvb = non-volatile binder volume
  CPVC = 1/ 1+ (OA)(ρ)/93.5
  OA = oil absorption (g linseed oil/g pigment)
  ρ = density of pigment
  93.5 = 100*density of linseed oil
  binder
  pigment
  CPVC
  voids
PVC vs. Film Properties

## Slide 9: Variations on the Formula
0.6 PVC/CPVC
0.6 PVC/CPVC
0.75 PVC/CPVC
Zinc Oxide

## Slide 10: Method for Evaluating Tensile and Elongation
Max Strain (Tensile)
Break %
(Elongation)
Load (lbf)
Instron Display:
Load vs. Displacement
Displacement (Inches)

## Slide 11: Film Thickness Matters
Tensile Strength
Chart: Max Strain, PSI
| A | B | C
0.01" | 300 | 183.5 | 415.1
0.02" | 210 | 110.1 | 291.7
Chart: Break %
| A | B | C
0.01" | 319.3 | 795.8 | 32.7
0.02" | 523.4 | 1106 | 27.8
Percent Elongation

## Slide 12: Tensile Strength is Impacted by Extender Particle Size
Chart: Particle Size, μm
| 0.7 | 3 | 4.3 | 12 | 3 | 11 | 2.4 | 8.6999999999999993 | 17 | 34 | 2.5 | 28 | 1.2 | 3 | 3.5
Avg. Max Str PSI | 285.8 | 235.47 | 199.2 | 179.04 | 194.09 | 142.81 | 225.15 | 186.4 | 203.11 | 197.62 | 232.21 | 182.17 | 298.4 | 349.4 | 247.5
0.6 PVC/CPVC, with Zinc Oxide
Tensile vs. Particle Size

## Slide 13: Tensile Strength is Impacted by Extender Particle Size
0.6 PVC/CPVC, with Zinc Oxide
Tensile vs. Extender Type
Chart: Max Strain, PSI
| 3μm | 12μm | 3μm | 11μm | 2.4μm | 8.7μm | 17μm | 34μm | 2.5μm | 28μm | 1.2μm | 3μm | Calcium Carbonate | Nepheline Syenite | Silica | Muscovite Mica | Wollastonite | Talc
Avg. Max Str PSI | 235.47 | 179.04 | 194.09 | 142.81 | 225.15 | 186.4 | 203.11 | 197.62 | 232.21 | 182.17 | 298.4 | 349.4

## Slide 14: Tensile Strength is Impacted by Extender Particle Size
Chart: Max Strain, PSI
| 0.7μm | 3μm | 4.3μm | 12μm | 19μm | Calcium Carbonate
Avg. Break % Stn | 285.8 | 235.47 | 199.2 | 179.04 | 164.9
Increasing PVC, Film Thickness
0.6 PVC/CPVC, with Zinc Oxide
Tensile vs. Particle Size

## Slide 15: Tensile Strength Increases with Increased PVC
Chart: Tensile vs. PVC
| 12 μm Calcium Carbonate | 3 μm Nepheline Syenite | 2.4 μm Silica | 0.6 μm Kaolin | 2.5 μm Wollastonite | 1.2 μm Talc | 12 μm Calcium Carbonate
37 PVC | 205.2 | 245.1 | 238.8 | 308.4 | 316.5 | 333.4
50 PVC | 273.5 | 335.7 | 392.8 | 545.8 | 501.2 | 558.9

## Slide 16: Elongation Does Not Correlate Well with Extender Particle Size
Chart: Particle Size, μm
| 0.7 | 3 | 4.3 | 12 | 3 | 11 | 2.4 | 8.6999999999999993 | 17 | 34 | 2.5 | 28 | 1.2 | 3 | 3.5
Avg. Break % Stn | 666.8 | 308.8 | 473 | 264.2 | 794.2 | 723.5 | 679 | 733 | 833.9 | 658.5 | 750.6 | 736.9 | 614.6 | 618.7 | 688
0.6 PVC/CPVC, with Zinc Oxide
Elongation vs. Particle Size

## Slide 17: Elongation Does Not Correlate Well with Extender Particle Size
Chart: Break %
| 0.7μm | 3μm | 4.3μm | 12μm | 19μm | Calcium Carbonate
Avg. Break % Stn | 666.8 | 308.8 | 473 | 264.2 | 352.2
0.6 PVC/CPVC, with Zinc Oxide
Elongation vs. Particle Size
Increasing PVC, Film Thickness

## Slide 18: Elongation Decreases with Increased PVC
Chart: Elongation vs. PVC
| 12 μm Calcium Carbonate | 3 μm Nepheline Syenite | 2.4 μm Silica | 0.6 μm Kaolin | 2.5 μm Wollastonite | 1.2 μm Talc | 12 μm Calcium Carbonate
37 PVC | 543 | 607.7 | 646.9 | 407.1 | 180.9 | 243.2
50 PVC | 124 | 101 | 54.9 | 46.07 | 36.7 | 46.5

## Slide 19: Tensile Strength Increases with the Inclusion of Zinc Oxide
Tensile vs. Extender Type
Chart: Max Strain, PSI
| 3μm | 3μm | 2.4μm | 17μm | 2.5μm | 1.2μm | Calcium Carbonate | Nepheline Syenite | Silica | Muscovite Mica | Wollastonite | Talc
Zinc, 0.6 PVC/CPVC | 235.47 | 194.09 | 225.15 | 203.11 | 232.21 | 298.4
No Zinc, 0.6 PVC/CPVC | 115.2 | 93.2 | 140.5 | 96.09 | 171.3 | 186.8

## Slide 20: Elongation Decreases with the Inclusion of Zinc Oxide
Elongation vs. Extender Type
Chart: Break %
| 3μm | 3μm | 2.4μm | 17μm | 2.5μm | 1.2μm | Calcium Carbonate | Nepheline Syenite | Silica | Muscovite Mica | Wollastonite | Talc
Zinc, 0.6 PVC/CPVC | 308.8 | 794.2 | 679 | 833.9 | 750.6 | 614.6
No Zinc, 0.6 PVC/CPVC | 997 | 1685 | 1175 | 1781 | 1089 | 1076

## Slide 21: Tensile Strength Increases with Increasing Fraction of Critical
Tensile vs. Extender Type
Chart: Max Strain, PSI
| 3μm | 3μm | 2.4μm | 17μm | 2.5μm | 1.2μm | Calcium Carbonate | Nepheline Syenite | Silica | Muscovite Mica | Wollastonite | Talc
No Zinc, 0.6 PVC/CPVC | 115.2 | 93.2 | 140.5 | 96.09 | 171.3 | 186.8
No Zinc, 0.75 PVC/CPVC | 303.25 | 139.5 | 188.3 | 124.4 | 329.6 | 254

## Slide 22: Elongation Decreases with Increasing Fraction of Critical
Elongation vs. Extender Type
Chart: Break %
| 3μm | 3μm | 2.4μm | 17μm | 2.5μm | 1.2μm | Calcium Carbonate | Nepheline Syenite | Silica | Muscovite Mica | Wollastonite | Talc
No Zinc, 0.6 PVC/CPVC | 997 | 1685 | 1175 | 1781 | 1089 | 1076
No Zinc, 0.75 PVC/CPVC | 28.6 | 827.43 | 733.1 | 921.4 | 210.1 | 633.7

## Slide 23: Balancing Tensile and Elongation
0.6 PVC/CPVC, with Zinc Oxide
Tensile and Elongation vs. Extender Type
Chart: Mechanical Values
| 3μm | 3μm | 2.4μm | 17μm | 2.5μm | 1.2μm | Calcium Carbonate | Nepheline Syenite | Silica | Muscovite Mica | Wollastonite | Talc
Tensile, PSI | 235.47 | 194.09 | 225.15 | 203.11 | 232.21 | 298.4
Elongation, Break % | 308.8 | 794.2 | 679 | 833.9 | 750.6 | 614.6

## Slide 24: Balancing Tensile and Elongation Removing Zinc Favors Elongation
0.6 PVC/CPVC, without Zinc Oxide
Tensile and Elongation vs. Extender Type
Chart: Mechanical Values
| 3μm | 3μm | 2.4μm | 17μm | 2.5μm | 1.2μm | Calcium Carbonate | Nepheline Syenite | Silica | Muscovite Mica | Wollastonite | Talc
Tensile, PSI | 119.6 | 80.1 | 101.25 | 81.625 | 167.4 | 162.8
Elongation, Break % | 1539 | 2000 | 2000 | 2000 | 1369.5 | 1198.5

## Slide 25: Balancing Tensile and Elongation Higher PVC/CPVC Restores Tensile Strength
0.75 PVC/CPVC, without Zinc Oxide
Tensile and Elongation vs. Extender Type
Chart: Mechanical Values
| 3μm | 3μm | 2.4μm | 17μm | 2.5μm | 1.2μm | Calcium Carbonate | Nepheline Syenite | Silica | Muscovite Mica | Wollastonite | Talc
Tensile, PSI | 303.25 | 139.5 | 188.3 | 124.4 | 329.6 | 254
Elongation, Break % | 28.6 | 827.43 | 733.1 | 921.4 | 210.1 | 633.7

## Slide 26: Weathering Dramatically Alters Tensile and Elongation
Tensile Strength
Elongation
Chart: Max Str, PSI
| A | B | C | D
Unweathered | 361 | 358.1 | 249.8 | 277.7
Weathered | 739.4 | 677.5 | 690.7 | 769.6
Chart: Break %
| A | B | C | D
Unweathered | 283.6 | 296.3 | 758.6 | 747.5
Weathered | 168.9 | 168.17 | 216.9 | 165.9
0.6 PVC/CPVC, with Zinc Oxide
0.67 PVC/CPVC, without Zinc Oxide

## Slide 27: Coalescent Usage Impacts the Balance Adding Texanol Reduces Tensile Strength
Chart: Tensile Strength
| 12 μm Calcium Carbonate | 3 μm Nepheline Syenite | 2.4 μm Silica | 0.6 μm Kaolin | 2.5 μm Wollastonite | 1.2 μm Talc
No Texanol | 273.5 | 335.7 | 392.8 | 545.8 | 501.2 | 558.9
5% Texanol | 217.2 | 278.6 | 284.5 | 418.7 | 400.3 | 414.7
50 PVC

## Slide 28: Coalescent Usage Impacts the Balance Adding Texanol Increases Elongation
Chart: Elongation
| 12 μm Calcium Carbonate | 3 μm Nepheline Syenite | 2.4 μm Silica | 0.6 μm Kaolin | 2.5 μm Wollastonite | 1.2 μm Talc
No Texanol | 124 | 101 | 54.9 | 46.07 | 36.7 | 46.5
5% Texanol | 367.2 | 218.9 | 189.6 | 138.5 | 95 | 83.8
50 PVC

## Slide 29: Summary of Direct and Inverse Relationships
    Fraction of Critical
    PVC
    Zinc Oxide Level
    Weathering
    Coalescent Level
    Plasticizer Level
    Fraction of Critical
    PVC
    Zinc Oxide Level
Tensile
    Particle Size
Elongation

## Slide 30: Method for Evaluating Two Cycle Recovery
Stretched 1” on Instron, 5 min
Stretched 1” on Instron, 5 min
1st Cycle
Measured after 10 Minutes
Measured after 24 Hours
{
1 cm
2nd Cycle
Removed and allowed to rest
Initial marks made 1 cm apart
Measured after 10 Minutes
Measured after 24 Hours
Removed and allowed to rest
% Recovery = Initial/Final

## Slide 31: Recovery Improves with the Inclusion of Zinc Oxide
Chart: Percent Recovery
| 3μm Calcium Carbonate | 3μm Nepheline Syenite | 2.4μm Silica | 17μm Muscovite Mica | 2.5μm Wollastonite | 1.2μm Talc | 3μm Talc
Zinc, 0.6 PVC/CPVC | 85 | 87 | 91 | 73 | 74 | 71 | 67
No Zinc, 0.6 PVC/CPVC | 64.5161 | 66.6667 | 67.8161 | 57.1429 | 53.4188 | 60.6061 | 57.1429
24 Hours After Second Pull

## Slide 32: Recovery Improves with Decreasing Fraction of Critical
Chart: Percent Recovery
| 3μm Nepheline Syenite | 2.4μm Silica | 17μm Muscovite Mica | 2.5μm Wollastonite | 1.2μm Talc | 3μm Talc
No Zinc, 0.6 PVC/CPVC | 66.6667 | 67.8161 | 57.1429 | 53.4188 | 60.6061 | 57.1429
No Zinc, 0.75 PVC/CPVC | 56.35 | 59.715 | 49.39 | 50.64 | 49.39 | 50
24 Hours After Second Pull

## Slide 33: Variables Combine to Produce a Wide Range of Recovery Values
Chart: Percent Recovery
| 0.7μm Calcium Carbonate | 3μm Calcium Carbonate | 4.3μm Calcium Carbonate | 12μm Calcium Carbonate | 19μm Calcium Carbonate | 3μm Nepheline Syenite | 11μm Nepheline Syenite | 2.4μm Silica | 8.7μm Silica | 17μm Muscovite Mica | 34μm Muscovite Mica | 2.5μm Wollastonite | 28μm Wollastonite | 1.2μm Talc | 3μm Talc | 3.5μm Kaolin | 3μm Calcium Carbonate | 3μm Nepheline Syenite | 2.4μm Silica | 17μm Muscovite Mica | 2.5μm Wollastonite | 1.2μm Talc | 3μm Talc | 3μm Nepheline Syenite | 2.4μm Silica | 17μm Muscovite Mica | 2.5μm Wollastonite | 1.2μm Talc | 3μm Talc | Zinc, 0.6 PVC/CPVC | No Zinc, 0.6 PVC/CPVC | No Zinc, 0.75 PVC/CPVC
 | 78.46 | 84.54 | 86.96 | 86.96 | 86.96 | 86.96 | 86.96 | 90.91 | 90.91 | 72.75 | 72.75 | 74.175 | 68.97 | 71.43 | 66.67 | 76.92 | 64.5161 | 66.6667 | 67.8161 | 57.1429 | 53.4188 | 60.6061 | 57.1429 | 56.35 | 59.715 | 49.39 | 50.64 | 49.39 | 50
24 Hours After Second Pull

## Slide 34: Recovery Shows Trends by Particle Morphology
Chart: Percent Recovery
| 3μm Calcium Carbonate | 12μm Calcium Carbonate | 3μm Nepheline Syenite | 11μm Nepheline Syenite | 2.4μm Silica | 8.7μm Silica | 2.5μm Wollastonite | 28μm Wollastonite | 17μm Muscovite Mica | 34μm Muscovite Mica | 1.2μm Talc | 3μm Talc | 3.5μm Kaolin | Nodular | Acicular | Platy
 | 84.54 | 86.96 | 86.96 | 86.96 | 90.91 | 90.91 | 74.175 | 68.97 | 72.75 | 72.75 | 71.43 | 66.67 | 76.92
0.6 PVC/CPVC, with Zinc Oxide
Recovery vs. Extender Type

## Slide 35: Weathering Improves Recovery
Chart: Percent Recovery
| A | B | C | D | 24 Hours After Second Pull
Unweathered | 83.33 | 82.19 | 57.14 | 54.05
Weathered | 86.96 | 88.89 | 80 | 80
0.6 PVC/CPVC, with Zinc Oxide
0.67 PVC/CPVC, without Zinc Oxide
Recovery

## Slide 36: Summary of Direct and Inverse Relationships
    Zinc Oxide
    Weathering
    Nodular Extenders
    Acicular Extenders
    Platy Extenders
    Fraction of Critical
Recovery

## Slide 37: Method for Evaluating Dirt Pick-up Resistance
10 mil DD
Initial Y-Reflectance Measurements
30 Cycles on Scrub Machine
Iron Oxide Slurry Applied
% Reflectance Retained = Final/Initial
Final Y-Reflectance Measurements
Allowed to dry
Sits for 2 Hours
7 Day Dry
For Weathered DPUR, drawdowns are done on Aluminum Q-Panels and placed in the QUV for 3 Days UV/Condensation prior to testing.
Q

## Slide 38: Dirt Pick-up Resistance Improves with Decreasing Particle Size
DPUR vs. Particle Size
Chart: Particle Size, μm
| 0.7 | 3 | 12 | 3 | 11 | 2.4 | 8.6999999999999993 | 1.2 | 3
 | 88.7034 | 74.1375 | 62.3875 | 75.3221 | 71.5881 | 82.6884 | 72.7453 | 81.7601 | 82.2574
Chart: Percent Reflectance Retained
| 0.7μm | 3μm | 12μm | 3μm | 11μm | 2.4μm | 8.7μm | 1.2μm | 3μm | Calcium Carbonate | Nepheline Syenite | Silica | Talc
with zinc | 88.7034 | 74.1375 | 62.3875 | 75.3221 | 71.5881 | 82.6884 | 72.7453 | 81.7601 | 82.2574
0.6 PVC/CPVC, with Zinc Oxide
DPUR vs. Extender Type

## Slide 39: Dirt Pick-Up Resistance Worsens with the Inclusion of Zinc Oxide
DPUR vs. Extender Type
Chart: Percent Reflectance Retained
| 3μm | 2.4μm | 1.2μm | 3μm | Nepheline Syenite | Silica | Talc
Zinc, 0.6 PVC/CPVC | 75.3221 | 82.6884 | 81.7601 | 82.2574
No Zinc, 0.6 PVC/CPVC | 76.7636 | 86.3671 | 90.0504 | 90.5784

## Slide 40: Weathered Dirt Pick-up Resistance is Impacted by Extender Type
0.67 PVC/CPVC, without Zinc Oxide
0.7 μm
Calcium Carbonate
3.0 μm
Calcium Carbonate
1.2 μm
Talc

## Slide 41: Summary of Direct and Inverse Relationships
    Particle Size
    Zinc Oxide
Dirt Pick-up Resistance

## Slide 42: Exploring Further

## Slide 43: Selecting an Extender Package: Variables to Consider
Settling
Texture
Barrier Properties
Stability
Water Resistance
Elasticity
Strength
Exterior Durability
Rheology
Cost
Optical Properties

## Slide 44: Using Extenders to Target Desired Properties
Lower PVC/CPVC
Efflorescence Resistance
Elongation
Higher PVC/CPVC
Permeability
Recovery
Tensile Strength

## Slide 45: Using Extenders to Target Desired Properties
Zinc
Recovery
Tensile Strength
No Zinc
Efflorescence Resistance
Elongation
Stability
DPUR

## Slide 46: Using Extenders to Target Desired Properties
Calcium Carbonate
Lower Cost
Mica
Barrier Properties
Elongation
Tensile
Recovery

## Slide 47: Thank you for your attention!